GUIDE SPECIFICATION FOR DECRA-SEAL™ W/B NON-YELLOWING ACRYLIC SEALER FOR DECORATIVE CONCRETE

SECTION 03 05 00

COMMON WORK RESULTS FOR CONCRETE 

	Specifier Notes: This guide specification is written according to the Construction Specifications Institute (CSI) format. The section must be carefully reviewed and edited by the architect or engineer to meet the requirements of the project. Coordinate this section with other specification sections and the drawings.


	Specifier Notes:  DECRA-SEAL W/B is a non-yellowing, urethane/acrylic polymer-based, high solids, liquid sealer for decorative concrete. The product is clear, transparent and easy-to-apply. DECRA-SEAL W/B also offers greatly improved chemical resistance when compared to standard acrylic only based curing and sealing compounds. The product has been formulated to seal and protect decorative colored concrete by producing a hard, yet flexible, clear film. DECRA-SEAL W/B meets the very strict maximum VOC content limits of 200 g/L for sealers as required by certain California Air Pollution Control Districts, as well as the 400 g/L VOC maximum required by the U.S. EPA Architectural Coatings Rule. This product is specifically formulated for the residential decorative concrete market.  DECRA-SEAL W/B is designed for various applications, including exterior concrete surfaces, driveways, patios, swimming pool areas and exposed aggregate, as well as any exterior surface where protection and sealing of concrete is desired. The use of DECRA-SEAL W/B on any exterior concrete surface provides a durable, long-lasting finish that has improved resistance to chemicals, oil, grease, de-icing salts and abrasions.


PART 1 GENERAL

1.01
SECTION INCLUDES


A.
Surface preparation.


B.
Application of clear, acrylic sealer for decorative concrete.
1.02
RELATED SECTIONS

	Specifier Notes: Edit the list of related sections as required for the project. List other sections dealing with work directly related to this section.



A.
Section 03 30 00 - Cast-in-Place Concrete. 

1.03
REFERENCES

A.
ASTM C1315 - Standard Specification for Liquid Membrane-Forming Compounds Having Special Properties for Curing and Sealing Concrete.

B.
U.S. Environmental Protection Agency Architectural Coatings Rule.

C.
California Air Pollution Control Districts VOC Level.

1.04
SUBMITTALS

A.
Comply with Section 01330 - Submittal Procedures. 


B.
Submit manufacturer's product data and application instructions. 
1.05
DELIVERY, STORAGE, AND HANDLING

A.
Deliver materials to site in manufacturer's original, unopened containers and packaging, with 
labels clearly identifying product name and manufacturer. 


B.
Store materials in a clean dry area in accordance with manufacturer's instructions.


C.
Keep product from freezing.

D.
Avoid direct contact with this product as it may cause mild to moderate irritation of the eyes and/or skin.

E.
Protect materials during handling and application to prevent damage or contamination.

F.
Do not mix any compound containing solvent.

1.06
ENVIRONMENTAL REQUIREMENTS

A.
Do not apply product when air, surface, or material temperatures are expected to fall below 40o F (4o C) within four hours of expected application.

B.
Do not apply to frozen concrete.

C.
Do not use on dense or porous surfaces.

PART 2
 PRODUCTS

2.01
MANUFACTURER

A.
W. R. MEADOWS®, INC., PO Box 338, Hampshire, Illinois 60140-0338. (800) 342-5976. (847) 683-4500. Fax (847) 683-4544. Web Site www.wrmeadows.com.

2.02
MATERIALS

A.
Performance Based Specification:  Water-based sealer shall be a non-yellowing, urethane/acrylic, polymer-based, high solids product having the following characteristics:

1.
ASTM C1315
Ultraviolet Resistance – Class A - Non-yellowing




Chalk Resistance – No chalking




Check/Peel Resistance – No deterioration

2.
Dried film accepted by USDA.

3.
Meets the maximum VOC content limits of 400 g/L for Concrete Sealers as required by the U.S. EPA Architectural Coatings Rule.

4.
Meets the California Air Pollution Control Districts maximum VOC level of 200 g/L.

B.
Proprietary Based Specification:  DECRA-SEAL W/B Non-Yellowing Acrylic Sealer for Decorative Concrete by W. R. MEADOWS.  

PART 3 EXECUTION

3.01
EXAMINATION

A.
Examine surfaces to receive sealer. Notify architect if surfaces are not acceptable. Do not begin surface preparation or application until unacceptable conditions have been corrected.

3.02
SURFACE PREPARATION


A.
Protect adjacent surfaces not designated to receive sealer.

B. 
Clean and prepare surfaces to receive sealer in accordance with manufacturer's instructions, ensuring that all stains, oil, grease, form release agents, dust and dirt are removed prior to application.


C. 
Ensure surface is clean and free from all powdered release agent residue.

D.
Apply sealer when surface water has completed disappeared on new concrete.

3.03
APPLICATION


A.
Apply sealer in accordance with manufacturer's instructions.

B.
Ensure product is mixed for optimum performance.

C.
Use industrial sprayer with an 5916 tip that produces a flow rate of 1/10 of one gallon per minute.

D.
Avoid puddling in low areas.

3.04
PROTECTION


A.
Restrict foot traffic for at least six hours; 12 hours is preferable.

END OF SECTION
Project Name 12/18/2007
03 05 00-3
Common Work Results for Concrete

